## Slide 1: Toyo Ink America’s Pressure Sensitive Adhesives for High Solids HVAC (HT & CT Technology) -2021
Good peel performance at RT / -10F.
  Acceptable at -20F
Excellent shear performance (meet UL-181L)
High solid 1 part PSA
Aluminum Foil Tape
Application
PSA |  | NXT-561 | NXT-562 | NXT-564 | NXT-566 | Target
Concept |  | STD | Good -10F peel | Good RT peel | Improved Peel Retention! High Shear | -
Solid content |  | 48% | 48% | 48% | 45% | -
Viscosity (mPa･s) |  | 6,000 | 6,000 | 4,500 | 4,500 | -
Type |  | 1 part | 1 part | 1 part | 1 part | -
15min Peel to SS (oz/inch) | at RT | 67 | 60 | 74 | 79 | 66
 | at -10F | 5 | 14 | 2 | 3 | -
Shear | 65℃-5lb-6hr | Pass | Pass | Pass | Pass | 6Hr OK
 | RT-10lb-120hr | Pass | Pass | Pass | Pass | 120Hr OK
[Condition]
Layer construction : AL-foil 50μm / PSA 65g/m2 / Paper release liner
Coating method : Transfer coating / 120C-5min drying
Aging : 23C-50%RH for 3 days