**AQUALESS PROCESS INK SERIES**

**Product Overview**

Aqualess high quality sheet-fed waterless printing inks for both DI and conventional presses. Its advantages include higher gloss, faster setting time, and improved transferability.

**Features**

\* Fast turn–around waterless-print

\* High dot fidelity printing

\* Quick color achievement

\* Ultrafast drying

\* Color and dot consistency batch to batch

\* Cobalt free

\* PFAS free

**Manufacturing Specifications**

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | ***Yellow*** | ***Magenta*** | ***Cyan*** | ***Black*** |
| **Medium Tack** |  |  |  |  |
| Tack\*1 | 16+/-0.5 | 16+/-0.5 | 16+/-0.5 | 17+/-1.0 |
| Vis\*2 | 1200+/-100 | 1200+/-200 | 1100+/-200 | 1200+/-200 |
| Flow\*3 | 15+/-1.00 | 15+/-1.00 | 15+/-1.00 | 15+/-1.00 |
| **Low Tack** |  |  |  |  |
| Tack\*1 | 15+/-0.5 | 16+/-0.5 | 16+/-0.5 | 16+/-0.5 |
| Vis\*2 | 1200+/\_50 | 1200+/\_50 | 1200+/-100 | 1200+/-150 |
| Flow\*3 | 15.5+/-0.5 | 15.5+/-0.5 | 15.5+/-0.5 | 15.5+/-0.5 |

\*1 Ink-O-Meter @800rpm, 90°F

\*2 Spread-O-Meter Radius(mm) @77°F

\*3 Viscosity: Haake RT20 @77F (in Poise)

Actual tack on the press varies due to ink film thickness, image area, press speed, fountain solution, and the condition of the press and press room. The merchandise contained herein is sold without warranties express or implied.

These conditions shall not be waived other than by an offer of the seller in writing.

Shelf life: Approximately 1 year

**Packaging**

Cans: 5 lbs.